# Supporting Information

Synthesis of mesogenic phthalocyanine-C60 donor–acceptor dyads designed for molecular heterojunction photovoltaic devices

# Yves Henri Geerts*1, Olivier Debever1, Claire Amato1, Sergey Sergeyev*1,2

Address: 1Université Libre de Bruxelles (ULB), Laboratoire de Chimie des Polymères, CP 206/01, Boulevard du Triomphe, 1050 Bruxelles, Belgium 2University of Antwerp, Department of Chemistry, Groenenborgerlaan 171, 2020 Antwerp, Belgium

Email: Sergey Sergeyev - serguei.sergueev@ua.ac.be; Yves Henri Geerts - ygeerts@ulb.ac.be

# Description of Supporting Information

1. Experimental details and spectra

2. Additional illustrations explaining the distribution of phthalocyanines resulting from the statistical condensations of phthalonitriles

3. Original 1H NMR spectra of 2c, 4c, and 1

4. Original 13C NMR spectra of 2c, 4c, and 1

5. Original MALDI-TOF spectra of 2c

4-(6-Hydroxyhexyloxy)phthalonitrile (6a). Prepared similarly to 5 from 6-bromohexan-1-ol (290 mg, 1.6 mmol), 7 (460 mg, 2 mmol), and K2CO3 (360 mg, 2.6 mmol) in dry DMF (15 mL). Yield 336 mg (86%). Light yellow solid; mp 65 °C; Rf = 0.41 (CH2Cl2); 1H NMR (300 MHz, CDCl3, 25 °C): 7.74 (d, 3JH,H = 8.8 Hz, 1H), 7.30 (d, 4JH,H = 2.6 Hz, 1H), 7.24 (dd, 3JH,H = 8.8 Hz, 4JH,H = 2.6 Hz, 1H), 4.09 (t, 3JH,H = 6.4 Hz, 2H, CH2OAr), 3.67 (t, 3JH,H = 6.6 Hz, 2H, CH2OH), 1.86 (quint, 3JH,H = 6.7, 2H), 1.37–1.67 (m, 6H), 1.33 (br, 1H, OH); 13C NMR (75 MHz, CDCl3, 25 °C): 162.1, 135.2, 119.4, 119.3, 117.4, 115.7, 115.2, 107.0, 69.1, 62.7, 32.7, 28.7, 25.6, 25.4; HR-MS (EI): m/z calcd. for C14H16N2O2 ([M]+): 244.1212, found: 244.1205.

4-(8-Hydroxyoctyloxy)phthalonitrile (6b). Prepared similarly to 6a from 8-bromooctan-1-ol (334 mg, 1.6 mmol). Yield 375 mg (81%). Light yellow solid; mp 61 °C; Rf 0.40 (CH2Cl2); 1H NMR (300 MHz, CDCl3, 25 °C):  7.68 (d, 3JH,H = 8.7 Hz, 1H), 7.25 (d, 4JH,H = 2.5 Hz, 1H), 7.18 (dd, 3JH,H = 8.8 Hz, 4JH,H = 2.6 Hz, 1H), 4.03 (t, 3JH,H = 6.5 Hz, 2H, CH2OAr), 3.59 (t, 3JH,H = 6.6 Hz, 2H, CH2OH), 1.79 (quint, 3JH,H = 6.9 Hz, 2H), 1.32–1.61 (m, 10H), signal of OH was not detected due to overlap with other signals; 13C NMR (75 MHz, CDCl3, 25 °C):  162.0, 135.0, 119.5, 119.2, 116.9, 115.6, 115.2, 106.4, 69.1, 62.4, 32.3, 29.0, 28.9, 28.4, 25.5, 25.4; HR-MS (EI): m/z calcd. for C16H20N2O2 ([M]+): 272.1525, found 272.1534.

4-(10-Hydroxydecyloxy)phthalonitrile (6c). Prepared similarly to 6a from 10-bromodecan-1-ol (380 mg, 1.6 mmol). Yield 399 mg (83%). Light yellow solid; mp 59 °C; Rf 0.43 (CH2Cl2); 1H NMR (300 MHz, CDCl3, 25 °C):  7.68 (d, 3JH,H = 8.8 Hz), 7.24 (d, 4JH,H = 2.6 Hz), 7.16 (dd, 3JH,H = 8.8 Hz, 4JH,H = 2.6 Hz, 1H), 4.03 (t, 3JH,H = 6.4 Hz, 2H, CH2OAr), 3.63 (t, 3JH,H 6.6 Hz, 2H, CH2OH), 1.81 (quint, 3JH,H = 6.7 Hz, 2H), 1.23–1.63 (m, 14H), signal of OH was not detected due to overlap with other signals; 13C NMR (75 MHz, CDCl3, 25 °C):  162.1, 135.2, 119.4, 119.3, 117.4, 115.7, 115.2, 107.0, 69.1, 62.7, 32.7, 29.7, 29.5, 29.3, 29.2, 28.7, 26.2, 25.8; HR-MS (EI): m/z calcd. for C18H24N2O2 ([M]+): 300.1838, found 300.1845.

4-[12-(Hydroxy)dodecyloxy]phthalonitrile (6d). Prepared similarly to 6a from 12-bromododecan-1-ol (424 mg, 1.6 mmol). Yield 420 mg (80%). Light yellow solid; mp 64 °C; Rf 0.44 (CH2Cl2); 1H NMR (300 MHz, CDCl3, 25 °C):  7.68 (d, 3JH,H = 8.8 Hz, 1H), 7.24 (d, 4JH,H = 2.6 Hz, 1H), 7.16 (dd, 3JH,H = 8.8 Hz, 4JH,H = 2.6 Hz, 1H), 4.03 (t, 3JH,H = 6.4 Hz, 2H, CH2OAr), 3.63 (t, 3JH,H = 6.6 Hz, 2H, CH2OH), 1.81 (quint, 3JH,H = 6.7 Hz, 2H), 1.23–1.63 (m, 18H), signal of OH was not detected due to overlap with other signals; 13C NMR (75 MHz, CDCl3, 25 °C):  162.2, 135.4, 119.4, 119.2, 117.5, 115.6, 115.2, 107.1, 69.2, 62.7, 32.4, 29.7, 29.5, 29.4, 29.2, 28.7, 26.4, 26.2, 25.8, 25.7; HR-MS (EI): m/z calcd. for C20H28N2O2 ([M]+) 328.2151, found 328.2139.

4-{6-[(2-Methoxyethoxy)methoxy]hexyloxy}phthalonitrile (9a). Prepared similarly to 9c from phthalonitrile 6a (100 mg, 0.41 mmol), MEMCl (0.1 mL; 0.83 mmol) and i-Pr2EtN (0.17 mL, 1.00 mmol) in CH2Cl2 (9 mL). Yield 124 mg (91%). Column chromatography of the residue afforded 9a (124 mg, 91%) as a light yellow solid; mp 46 °C; Rf 0.69 (CH2Cl2/AcOEt 4 : 1). 1H NMR (300 MHz, CDCl3, 25 °C):  7.68 (d, 3JH,H = 8.8 Hz, 1H), 7.24 (d, 4JH,H = 2.6 Hz, 1H), 7.14 (dd, 3JH,H = 8.8 Hz, 4JH,H = 2.6 Hz, 1H), 4.69 (s, 2H, OCH2O), 4.03 (t, 3JH,H = 6.5 Hz, 2H, CH2O), 3.68 (t, 3JH,H = 5.0 Hz, 2H, CH2O), 3.52–3.60 (m, 4H, OCH2CH2O), 3.38 (s, 3H, MeO), 1.81 (quint, 3JH,H = 7.2 Hz, 2H), 1.27–1.63 (m, 6H); 13C NMR (75 MHz, CDCl3, 25 °C):  162.2, 135.1, 119.5, 119.3, 117.4, 115.7, 115.3, 107.0, 95.5, 71.8, 69.3, 67.9, 66.7, 59.0, 29.7, 29.4 , 28.7, 26.2; HR-MS (EI): m/z calcd. for C18H24N2O4 ([M]+) 332.1736, found 332.1721.

4-{8-[(2-Methoxyethoxy)methoxy]octyloxy}phthalonitrile (9b). Prepared similarly to 9c from phthalonitrile 6a (400 mg, 1.47 mmol), MEMCl (0.33 mL, 2.94 mmol) and i-Pr2EtN (0.77 mL, 4.5 mmol) in CH2Cl2 (30 mL). Yield 471 mg (89%). Light yellow solid; mp 41 °C; Rf 0.67 (CH2Cl2/AcOEt 4 : 1). 1H NMR (300 MHz, CDCl3, 25 °C):  7.68 (d, 3JH,H = 8.8 Hz, 1H), 7.24 (d, 4JH,H = 2.6 Hz, 1H), 7.14 (dd, 3JH,H = 8.8 Hz, 4JH,H = 2.6 Hz, 1H), 4.69 (s, 2H, OCH2O), 4.03 (t, 3JH,H = 6.5 Hz, 2H, CH2O), 3.68 (t, 3JH,H = 5.0 Hz, 2H, CH2O), 3.52–3.60 (m, 4H, OCH2CH2O), 3.38 (s, 3H, MeO), 1.81 (quint, 3JH,H = 7.2 Hz, 2H), 1.27–1.63 (m, 10H); 13C NMR (75 MHz, CDCl3, 25 °C):  162.0, 135.0, 119.4, 119.1, 117.0, 115.6, 115.1, 106.5, 95.1, 71.6, 69.0, 67.6, 66.4, 58.7, 29.3, 29.0, 28.9, 28.4, 25.8, 25.4; HR-MS (ESI): m/z calcd. for C20H28N2O4 ([M+Na]+): 383.1947, found 383.1935.

4-{12-[(2-Methoxyethoxy)methoxy]dodecyloxy}phthalonitrile (9d). Prepared similarly to 9c from phthalonitrile 6d (285 mg, 0.74 mmol), MEMCl (0.17 mL, 1.47 mmol) and i-Pr2EtN (0.39 mL, 2.25 mmol) in CH2Cl2 (15 mL). Yield 286 mg (93%). Light yellow solid; mp 39 °C; Rf 0.62 (CH2Cl2/AcOEt 9 : 1); 1H NMR (300 MHz, CDCl3, 25 °C):  7.68 (d, 3JH,H = 8.8 Hz, 1H), 7.24 (d, 4JH,H = 2.6 Hz, 1H), 7.14 (dd, 3JH,H = 8.8 Hz, 4JH,H = 2.6 Hz, 1H), 4.69 (s, 2H, OCH2O), 4.03 (t, 3JH,H = 6.5 Hz, 2H, CH2O), 3.68 (t, 3JH,H =5.0 Hz, 2H, CH2O), 3.52–3.60 (m, 4H, OCH2CH2O), 3.38 (s, 3H, MeO), 1.81 (quint, 3JH,H = 7.2 Hz, 2H), 1.27–1.63 (m, CH2, 18H); 13C NMR (75 MHz, CDCl3, 25 °C):  162.2, 135.1, 119.5, 119.3, 117.4, 115.7, 115.3, 107.0, 95.5, 71.8, 69.3, 67.9, 66.7, 59.0, 29.7, 29.4, 29.4, 29.4, 29.3, 29.3, 29.2, 28.7, 26.2, 25.8; HR-MS (ESI): m/z calcd. for C24H36N2O4 ([M+Na]+) 439.2573, found 439.2570.

2-{6-[(2-Methoxyethoxy)methoxy]hexyloxy}-9(10),16(17),23(24)-tri(2-decyltetradecyloxy)-29H,31H-phthalocyanine (10a). Prepared similarly to 10c from 5 (2.93 g, 6.1 mmol), 9a (225 mg, 0.68 mmol) and Li (105 mg, 15 mmol) in n-pentanol (15 mL). Yield of 10a 157 mg (13%). Green solid; Rf 0.75 (CH2Cl2/AcOEt 1 : 1); 1H NMR (300 MHz, CDCl3, 25 °C):  8.50–8.90 (m, 4H), 8.10–8.50 (m, 4H), 7.30–7.55 (m, 4H), 4.82 (s, 2H, OCH2O), 4.28–4.57 (m, 8H, ArOCH2), 3.67–3.80 (m, 4H, CH2OCH2OCH2), 3.58–3.63 (m, 2H, OCH2CH2O), 3.42 (s, 3H, MeO), 2.05–2.20 (m, 5H, ArOCH2CH2 + ArOCH2CH), 1.15–1.90 (m, 126H), 0.87 (t, 3JH,H =7.0 Hz, 18H), –2.76 (br, 2H, NH); HR-MS (MALDI): m/z calcd. for C114H182N8O7 ([M]+) 1775.4132, found 1775.4167.

2-{8-[(2-Methoxyethoxy)methoxy]octyloxy}-9(10),16(17),23(24)-tri(2-decyltetradecyloxy)-29H,31H-phthalocyanine (10b). Prepared similarly to 10c from 5 (3.41 g, 7.1 mmol), 9b (284 mg, 0.79 mmol), Li (125 mg, 17.7 mmol), and pentanol (25 mL). Yield of 10b 299 mg (21%). Green solid; Rf 0.75 (CH2Cl2/AcOEt 1 : 1). 1H NMR (300 MHz, CDCl3, 25 °C):  8.50–8.90 (m, 4H), 8.10–8.50 (m, 4H), 7.30–7.60 (m, 4H), 4.82 (s, 2H, OCH2O), 4.28–4.54 (m, 8H, ArOCH2), 3.65–3.80 (m, 4H, CH2OCH2OCH2), 3.58–3.63 (m, 2H, OCH2CH2O), 3.45 (s, 3H, MeO), 2.07–2.20 (m, 5H, ArOCH2CH2 + ArOCH2CH), 1.15–1.90 (m, 130H), 0.92 (t, 3JH,H =7.0 Hz, 18H), –2.91 (s, 2H, NH). HR-MS (MALDI): m/z calcd. for C116H186N8O7 ([M]+) 1803.4445, found 1803.4220

2-{12-[(2-Methoxyethoxy)methoxy]dodecyloxy}-9(10),16(17),23(24)-tri(2-decyltetradecyloxy)-29H,31H-phthalocyanine (10d). Prepared similarly to 10c from 5 (3.41 g, 7.1 mmol), 9d (330 mg, 0.79 mmol), Li (125 mg, 17.7 mmol), and pentanol (25 mL). Yield of 10d 264 mg (18%). Green solid; Rf 0.75 (CH2Cl2/AcOEt 1 : 1). 1H NMR (300 MHz, CDCl3, 25 °C):  8.50–8.90 (m, 4H), 8.10–8.50 (m, 4H), 7.30–7.60 (m, 4H), 4.76 (s, 2H, OCH2O), 4.25–4.52 (m, 8H, ArOCH2), 3.65–3.80 (m, 4H, CH2OCH2OCH2), 3.58–3.63 (m, 2H, OCH2CH2O), 3.45 (s, 3H, MeO), 2.10–2.23 (m, 5H, ArOCH2CH2 + ArOCH2CH), 1.15–1.90 (m, 138H), 0.88 (t, 3JH,H = 6.8 Hz, 18H), –2.26 (s, 2H, NH); HR-MS (MALDI): m/z calcd. for C120H194N8O7 ([M]+) 1859.5071, found 1859.5079.

2-(6-Hydroxyhexyloxy)-9(10),16(17),23(24)-tri(2-decyltetradecyloxy)-29H,31H-phthalocyanine (4a). Prepared similarly to 4c from 10a (266 mg, 0.15 mmol). Yield 253 mg (100%). Green solid; 1H NMR (300 MHz, CDCl3, 25 °C):  8.90–9.20 (m, 4H), 8.45–8.80 (m, 4H), 7.50–7.75 (m, 4H), 4.35–4.55 (m, 8H, ArOCH2), 3.78 (t, 3JH,H = 6.0 Hz, 2H, CH2OH), 2.05–2.20 (m, 5H, ArOCH2CH2 + ArOCH2CH), 1.10–1.95 (m, 126H), 0.75–0.95 (m, 18H), NH not observed; HR-MS (MALDI): m/z calcd. for C110H174N8O5 (([M]+): 1687.3607, found 1687.3147.

2-(8-Hydroxyoctyloxy)-9(10),16(17),23(24)-tri(2-decyltetradecyloxy)-29H,31H-phthalocyanine (4b). Prepared similarly to 4a from 10b (270 mg, 0.15 mmol). Yield 257 mg (100%). Green solid; 1H-NMR (300 MHz, CDCl3, 25 °C):  8.90–9.20 (m, 4H), 8.45–8.80 (m, 4H), 7.50–7.75 (m, 4H), 4.35–4.55 (m, 8H, ArOCH2), 3.80 (t, 3JH,H = 6.0 Hz, 2H, CH2OH), 2.03–2.20 (m, 5H, ArOCH2CH2 + ArOCH2CH), 1.10–1.95 (m, 130H), 0.79–0.93 (m, 18H), –3.10 (s, 2H, NH); HR-MS (MALDI): m/z calcd. for C112H178N8O5 ([M]+): 1715.3920, found 1715.4406.

2-(12-hydroxy-dodecyloxy)-9(10),16(17),23(24)-tri(2-decyltetradecyloxy)-29H,31H-phthalocyanine (4d). Prepared similarly to 4a from 10d (280 mg, 0.15 mmol). Yield 266mg (100%); Green solid; 1H-NMR (300 MHz, CDCl3, 25 °C):  8.90–9.20 (m, 4H), 8.45–8.80 (m, 4H), 7.50–7.75 (m, 4H), 4.35–4.55 (m, 8H, ArOCH2), 3.69 (t, 3JH,H = 6.0 Hz, 2H, CH2OH), 2.03–2.20 (m, 5H, ArOCH2CH2 + ArOCH2CH), 1.10–1.95 (m, 138H), 0.80–0.93 (m, 18H), –2.97 (s, 2H, NH); HR-MS (MALDI): m/z calcd. for C116H186N8O5 ([M]+): 1771.4546, found 1771.4551.

Phthalocyanine-C60 dyad 2a. Prepared similarly to dyad 2c starting from 4c (63 mg, 0.037 mmol). Yield 43 mg (45%). Viscous green liquid; Rf 0.64 (CH2Cl2/hexane 3 : 2); 1H-NMR (300 MHz, CDCl3, 25 °C):  8.25–8.80 (m, 4H), 7.90–8.20 (m, 4H), 7.79 (d, 3JH,H = 7.4 Hz, 2H), 7.35–7.55 (m, 7H), 4.20–4.50 (m, 8H, ArOCH2), 4.05–4.15 (m, 2H, COOCH2), 2.68 (t, 3JH,H = 7.5 Hz, 2H, CH2COO), 2.42 (t, 3JH,H = 7.0 Hz, 2H, PhCCH2), 1.95–2.25 (m, 7H, ArOCH2CH2 + ArOCH2CH + CH2CH2COO), 1.15–1.95 (m, 126H), 0.80–0.95 (m, 18H), –3.20 (s, 2H, NH); HR-MS (MALDI): m/z calcd. for C181H184N8O6 (([M]+): 2565.4339, found 2565.4316.

Phthalocyanine-C60 dyad 2b. Prepared similarly to dyad 2a starting from 4b (64 mg, 0.037 mmol). Yield 40 mg (42%). Viscous green liquid; Rf 0.60 (CH2Cl2/hexane 3 : 2); 1H-NMR (300 MHz, CDCl3, 25 °C):  8.25–8.80 (m, 4H), 7.90–8.20 (m, 4H), 7.70 (d, 3JH,H = 7.4 Hz, 2H), 7.30–7.60 (m, 7H), 4.20–4.50 (m, 8H, ArOCH2), 4.05–4.15 (m, 2H, COOCH2), 2.64 (t, 3JH,H = 7.5 Hz, 2H, CH2COO), 2.43 (t, 3JH,H = 7.0 Hz, 2H, PhCCH2), 1.95–2.25 (m, 7H, ArOCH2CH2 + ArOCH2CH + CH2CH2COO), 1.15–1.90 (m, 130H), 0.80–0.95 (m, 18H), –3.20 (s, 2H, NH); HR-MS (MALDI): m/z calcd. for C183H188N8O6 ([M]+): 2593.4652, found: 2593.5417.

Phthalocyanine-C60 dyad 2d. Prepared similarly to dyad 2a starting from 4d (66 mg, 0.037 mmol). Yield 39 mg (40%). Green solid; Rf 0.65 (CH2Cl2/hexane 3:2); 1H NMR (300 MHz, CDCl3, 25 °C):  8.25–8.80 (m, 4H), 7.90–8.20 (m, 4H), 7.78 (d, 3JH,H = 7.4 Hz, 2H), 7.30–7.60 (m, 7H), 4.20–4.50 (m, 8H, ArOCH2), 4.05–4.15 (m, 2H, COOCH2), 2.72 (t, 3JH,H = 7.5 Hz, 2H, CH2COO), 2.40 (t, 3JH,H = 7.0 Hz, 2H, PhCCH2), 1.98–2.25 (m, 7H, ArOCH2CH2 + ArOCH2CH + CH2CH2COO), 1.10–1.90 (m, 138H), 0.80–0.95 (m, 18H), –2.95 (s, 2H, NH); HR-MS (MALDI): m/z calcd. for C187H196N8O6 ([M]+): 2649.5278, found 2649.5444.

Figure SI1: Statistical condensation of the two dinitriles A and B leads to a mixture of phthalocyanines A4, A3B, A2B2, AB3 and B4.

Figure SI2: The distribution of phthalocyanines A4, A3B, A2B2, AB3 and B4 resulting from statistical condensation of the two dinitriles A and B can be described by the coefficients of a binom (3A + B)4 = 81A4 + 108A3B + 54A2B2 + 12AB3 + B4 (for the molar ratio A/B = 3 : 1) or (9A + B)4 = 6561A4 + 2916A3B + 486A2B2 + 36AB3 + B4 (for the molar ratio A/B = 9 : 1).

Figure SI3: Condensation of 3-substituted phthalonitrile A produces a statistical mixture of four regioisomeric phthalocyanines of different symmetry (C4h, D2h, C2v, Cs). Statistical condensation of the two 3-substituted dinitriles A and B produces A3B phthalocyanine as a mixture of eight regioisomers.

Figure SI4: 1H NMR spectrum of dyad 2c (300 MHz, 25 °C, 7.6∙10–3 M).

Figure SI5: 1H NMR spectrum of PCBM 1 (300 MHz, 25 °C, 2.2∙10–2 M).

Figure SI6:1H NMR spectrum of phthalocyanine 4c (300 MHz, 25°C, 1.15∙10–3 M).

Figure SI7: 13C NMR spectrum of dyad 2c (100 MHz, 25 °C, 3.05∙10–2 M).

Figure SI8: 13C NMR spectrum of PCBM 1 (75 MHz, 25 °C, 2.2∙10–2 M).

Figure SI9: 13C NMR spectrum of phthalocyanine 4c (100 MHz, 25 °C, 4.6∙10–2 M).

Figure SI10: MALDI-TOF mass spectrum of dyad 2c.