Supporting Information

for

A photochemical determination of luminescence efficiency of upconverting nanoparticles

Baptiste Amouroux, Clément Roux, Jean-Claude Micheau, Fabienne Gauffre, Christophe Coudret

Experimental details and characterization data

Table of contents

General procedure for the preparation of UCNP batch	S2

Characteristics of UCNP batch (stoichiometry, datas from TEM, datas from XRD)	S3

TEM analysis of UCNP batch	S4

XRD analysis of UCNP batch	S5

Discoloration of DAE induced by UCNP batch (S1)	S6

General procedure for the preparation of a second UCNP batch with a diameter of 35 nm	S7

Discoloration of DAE induced by 35nm-UCNP	S8

S2- Experimental section

Photochromic actinometer: 1,2-Bis(2,4-dimethyl-5-phenyl-3-thienyl)-3,3,4,4,5,5-hexafluoro-1-cyclopentene (≥98%, CAS: 172612-67-8) was obtained from TCI chemicals and used as received.

The molar extinction coefficient of 1-c at 540nmm was determined by normalizing a UV vis spectrum of a 1-o/1-c mixture using the published value at 562 nm1 (since only the 1-c form exist in this spectral range there is no need of determining its concentration

# Procedure for the preparation of UCNP batch

UCNP were prepared adapting the protocols of Li and Zhang2 and Zhai et al.3 Rare earth (RE) chloride hydrates were mixed in a oleic acid (OA): octadecene (ODE) (7:38) mixture and heated to 160°C under Ar flush until a clear solution was obtained. To the cooled reaction mixture were slowly added freshly prepared solutions of NaOH (0.326 mM) and NH4F (0.5 mM) in MeOH via syringe pump at 0.4 mL min-1. Volatile compounds were then removed under Ar flush then the reaction mixture iwa brought to 300-310 for 90 minutes. Timer was started when temperature reached 300°C. It should be noted that temperature never reached 310 but stayed at around 305°C.

# S3-Characteristics of UCNP batch (stoichiometry, datas from TEM, datas from XRD)

|  | UCNPs |
| --- | --- |
| Matrix | NaYF4 |
| n(RE) | 11.6 mmol |
| n(Y) | 7.9 mmol (68% RE) |
| n(Yb) | 3.5 mmol (30% RE) |
| n(Yb) | 0.23 mmol (2% RE) |
| n(Na)/n(RE) | 4 |
| n(F)/n(RE) | 5.5 |
| V(OA) mL | 35 |
| V(ODE) mL | 190 |
| {Na+F} addition | Separated addition via double syringe pump |
| Diameter | 21.8 nm |
| Area | 1.49 * 103 nm² |
| Volume | 5.42 * 103 nm3 |
| Unit cell volume U(NaYF4:Yb,Er) | 107.6 Å3 |
| Z | 1.5 |
| N(Yb/NP) | 22670 |
| N(Er/NP) | 1510 |

# S4-TEM analysis of UCNP batch

scale bar =100nm

UCNP synthesized are homogeneous in size and shape. We have assimilated them to a pseudo-sphere of a diameter of 21.8 ± 1.3 nm (average size ± FWHM)

# S5-XRD analysis of UCNP batch

XRD is consistent with the hexagonal phase

# S6-Discoloration of DAE induced by UCNP batch (S1)

DAE discoloration induced by UCNP under 976m CW laser at a power of 4.1W (49 W cm-2). Conditions are reported in the main text. The high absorbance ensures total light absorption at 540nm.

A convenient parameter is the characteristic “optical thickness”4 L defined from the rewritten Beer Lambert law: 
I=I010−lL

as
L=1ε5401c

L is therefore the inverse of the absorbance measured for an optical path of 1cm. Thus, an absorbance at 530nm of 2.1 (over 1cm) gives a characteristic length of 0.47 cm, comparable to the dimensions of the cuvette:

Quartz cell containing the mixture of DAE and UCNP (21.8nm) was placed in UV-visible spectrophotometer. Absorbance spectra were recorded in a kinetic mode, while the cell was irradiated from the side by a fibered collimated NIR laser.

# S7-General procedure for the preparation of a second UCNP batch with a diameter of 35 nm

NaYF4,Yb,Er UCNPs were prepared by applying the protocol described by Li and Zhang3, using a doping molar ratio of 80% Y, 18% Yb,  2% Er.

# S8-Summary table

| Step | parameter | symbol | unit | value |
| --- | --- | --- | --- | --- |
| Photolysis of 1-c | DAE 1-c concentration | [1-c] | mol L-1 | 2.12 × 10-4 |
|  | 1-c molar extinction coefficient at 650nm (monitoring) | 650 | L mol-1 cm-1 | 2154 |
|  | 1-c molar extinction coefficient at 540nm | 540 | L mol-1 cm-1 | 9784 |
|  | Volume of the DAE solution | V | L | 1.96 × 10-3 |
|  | DAE opening quantum yield at 540nm | CO | - | 0.02 |
|  | DAE Absorbance at 540 nm (irradiation) | Abs540 | - | 2.07 |
|  | Optical length at 540 nm | L | cm | 0.48 |
|  | Initial slope DAE photobleaching | -dAbs650/dt | Abs s-1 | 1.46 × 10-5 |
|  | DAE bleaching rate | -d[1-c]/dt | mol L-1 s-1 | 6.78 × 10-9 |
|  | DAE consumption |  | molecule s-1 | 8.00 × 1012 |
| Incoming NIR energy | Upconversion photon flux at 540nm | J0 | photon s-1 | 4.00 × 1014 |
|  | Laser power at 976 nm (NIR) | P | W | 4.7 |
|  | Laser power density at 976 nm (NIR) |  | W cm-2 | 49 |
|  | Incident NIR photon flux | J0NIR | photon s-1 | 2.31 × 1019 |
|  | Absorbance of UCNP solution at 976 nm | Abs976 | - | 0.0014 |
|  | Absorbed NIR photon flux | JaNIR | photon s-1 | 7.45 × 1016 |
|  | Up-conversion QY | UC | - | 0.54% |
| Single NP power | Laser beam section |  | cm2 | 9.6 × 10-2 |
|  | Laser beam volume inside the cell (“lamp”) | v | L | 9.6 × 10-5 |
|  | Yb molar extinction coefficient at 976 nm | Yb | L mol-1 cm-1 | 3.1 |
|  | number of Yb atoms inside the beam volume | nYb | atom | 2.58 × 1016 |
|  | Total number of RE per nanoparticle (from XRD) | NRE | atom NP-1 | 75490 |
|  | percentage of Yb | pYb | % | 30 |
|  | percentage of Er | pEr | % | 2 |
|  | number of ytterbium per nanoparticle | NYb | atom NP-1 | 22670 |
|  | number of erbium per nanoparticle | NEr | atom NP-1 | 1510 |
|  | number of NPs inside the laser beam | nYb | NP | 1.14 × 102 |
|  | emitted photons per erbium atom | J0/NEr | photon s-1 | 0.24 |
|  | number of emitted photons per NP’s | J0/nNP | photon s-1 | 350 |
|  | Power per NP’s | ℘NP | W | 1.29 × 1016 |

# S9-Discoloration of DAE induced by 35nm-UCNP

Photoizomerization of DAE induced by UCNP emission was monitored in diluted conditions : Abs(500-600nm)≈0.15. Complete kinetic is represented on top, while zoom-in of the region of interest (where only 1-c absorbs) is shown at the bottom.

In such conditions it is not possible to define simply the absorbed flux density [loubiere]. Thus, no quantum yield could be determined. Nevertheless, the activity of the nanolamp could be determined: in this geometry, one single 35nm-UCNP induces 20 dyes switching per second (ratio of the measured disappearance slope by the number of UCNP within the 976nm-irradiated volume).

# S10-References:

(1) 	Sumi, T.; Takagi, Y.; Yagi, A.; Morimoto, M.; Irie, M. Chemical Communications 2014, 50 (30), 3928–3930. https://doi.org/10.1039/C4CC00396A.

(2) 	Li, Z.; Zhang, Y. Nanotechnology 2008, 19 (34), 345606. https://doi.org/doi:10.1088/0957-4484/19/34/345606.

(3) 	Zhai, X.; Wang, Y.; Liu, X.; Liu, S.; Lei, P.; Yao, S.; Song, S.; Zhou, L.; Feng, J.; Zhang, H. ChemPhotoChem 2017, 1 (8), 369–375.

(4) 	Aillet, T.; Loubiere, K.; Dechy-Cabaret, O.; Prat, L. International Journal of Chemical Reactor Engineering 2014, 12 (1), 257–269. https://doi.org/10.1515/ijcre-2013-0121.