Supporting Information

Nickel nanoparticle decorated reduced graphene oxide-WO3 nanocomposite  - a promising candidate for gas sensing

Ilka Simon,[1] Alexandr Savitsky,[2] Rolf Mülhaupt,[3] Vladimir Pankov,*[2] and Christoph Janiak*[1]

Adresse:

1 Institut für Anorganische Chemie und Strukturchemie, Heinrich-Heine-Universität Düsseldorf, 40204 Düsseldorf, Germany. Fax: +49-211-81-12287; Tel: +49-211-81-12286.

Email: janiak@uni-duesseldorf.de

2 Chemical Faculty, Belarusian State University, Lenningradskaya str. 14, 220050 Minsk, Belarus

Email: Vladimir Pankov – pankov@bsu.by

3 Freiburg Materials Research Center and Institute for Macromolecular Chemistry, Albert-Ludwigs-University Freiburg, 79104 Freiburg, Germany

* Corresponding author

Ilka Simon: ilka.simon@uni-duesseldorf.de, ORCID-ID: 0000-0002-1143-4205

Alexandr Savitsky: aasavitsky@yandex.ru

Rolf Mülhaupt: rolf.muelhaupt@makro.uni-freiburg.de

Sensing materials – examples form literature

Table S1: Examples of metal oxide sensing elements from literature. (G = graphene, GO = graphene oxide,  rGO = reduced graphene oxide)

| Sensing material | Gas | Temperature | Response (%) | Response / recovery time | Reference |
| --- | --- | --- | --- | --- | --- |
| MOS |  |  |  |  |  |
| WO3 | 100 ppb NO2 | 140 °C |  |  | [] |
| Graphene+MOS |  |  |  |  |  |
| rGO@WO3 | 5 ppm NO2 | RT | 769 | 9 / 18 min | [] |
| WO3@G | 20 ppm, NO2 | 300 °C | 202 | - | [] |
| WO3@rGO | 5 ppm NO2 | 250 °C | 135 | 25 / 200 s | [] |
| MWCNTs@WO3 | 5 ppm NO2 | RT | 77 | 10.5 / 20 | [] |
| WO3@S-rGO | 20 ppm NO2 | RT | 149 | 6 s / 56 s | [] |
| WO3@rGO | 56 ppm NO2 | RT | 40.8 | 250 s | [] |
| WO3@G | 1 ppm NO2 |  | 96 | 0.42-3.3 / 0.42-3.3 | [4] |
| rGO@ZnO | 5 ppm NO2 | RT | 25.6 | 165 / 499 s | [] |
| GO@SnO2 | 200 ppm acetone |  | 200 |  | [] |
| SnO2@S-rGO | 20 ppm NO2 | RT | 26.3 | 40 / 357 s | [] |
| MOS+MOS |  |  |  |  |  |
| WO3/NiO | 50 ppm H2S | 250 °C | 50 | 4 / 66 s | [] |
| NiO/SnO2 | 200 ppm acetone | 150- 350 °C | 54.4 | 13 s /3 min | [] |
| NiO/SnO2 | 500 ppm acetone | 300 °C | 38 | 23 s / 1 min | [] |
| NiO/SnO2 | 100 ppm ethanol | 350 °C | 59 | 2s / 15 s | [] |
| NiO/SnO2 | 50 ppm butanol | 350 °C | 28 |  | [] |
| NiO/SnO2 | 0.5 ppm Ethanol | 350 °C | 50 |  | [] |
| NiO/SnO2 | 1000 ppm Acetone | 340 °C | 265 | 7 s / 30 s | [] |
| Al@NiO | 100 ppm ethanol | 200 °C | 1.9 -> 12.0 | Shorter time | [] |
| Ga@In2O3 | 100 ppm HYHO | 150 °C | 13.0 -> 52.4 | NA | [] |
| Au@WO3 | 5 ppm NO2 | 100 °C | Increased by 4 x | 218 -> 4 | [] |
| ternary systems |  |  |  |  |  |
| NiO/SnO2/G | 200 ppm acetone | 150-350 °C | 169.7 | 5.4 s / 2.5 min | [] |
| NiO/SnO2/rGO | 60 ppm NO2 | RT | 62.27 | 220 s / 835 s | [] |
| CuO/ZnO/rGO | 10 ppm acetone |  | 9.4 |  | [] |
| rGO/NiO/ZnO | 100 ppm Hydrogen | 150 °C | 63.8 | 28 s | [] |
| (InOx/SnO2)@rGO | 100 ppm NO2 | RT | 22 | 400 s | [] |
| FeOx/WO3/rGO | 3 ppm NO2 | RT | 5.9 | 1500 / 7200 s | [] |
| Ag/rGO/SnO2 | 5 ppm NO2 | RT | 2.17 | 49 / 339 s | [] |
| Pd@(rGO/TiO2) | 100 ppm Methanol | 50 °C | 72.14 | 69 / 72 s | [] |
| Pd@(rGO/MnO2) | 100 ppm methanol | 27 °C | 91.45 | 71 / 79 s | [28] |
| Pd@(rGO/WO3) | 100 ppm ethanol | 27 °C | 76.01 | 21 / 39 s | [28] |
| WO3/Pt@rGO | 10 ppm acetone | 200 °C | 12.2 | 14.1 / 16.8s | [] |
| Pd@(WO3/rGO) | 100 ppm H2 |  | 7200 | 0.59 / 0.61 | [] |

[] Li, J.; Liu, X.; Cui, J.; Sun, J. ACS Appl. Mater. & Interfaces 2015, 7 (19), 10108–10114. doi:10.1021/am508121p.

[] Su, P.-G.; Peng, S.-L. Talanta 2015, 132, 398–405. doi:10.1016/j.talanta.2014.09.034.

[] An, X.; Yu, J. C.; Wang, Y.; Hu, Y.; Yu, X.; Zhang, G. J. Mater. Chem. 2012, 22 (17), 8525–8531. doi:10.1039/c2jm16709c.

[] Srivastava, S.; Jain, K.; Singh, V. N.; Singh, S.; Vijayan, N.; Dilawar, N.; Gupta, G.; Senguttuvan, T. D. Nanotechnology 2012, 23 (20), 205501–205507. doi:10.1088/0957-4484/23/20/205501.

[] Su, P.-G.; Pan, T.-T. Materials Chemistry and Physics 2011, 125 (3), 351–357. doi:10.1016/j.matchemphys.2010.11.001.

[] Wang, T.; Hao, J.; Zheng, S.; Sun, Q.; Di Zhang; Wang, Y. Nano Res. 2018, 11 (2), 791–803. doi:10.1007/s12274-017-1688-y.

[] Jie, X.; Zeng, D.; Zhang, J.; Xu, K.; Wu, J.; Zhu, B.; Xie, C. Sens. Actuators, B 2015, 220, 201–209. doi:10.1016/j.snb.2015.05.047.

[] Liu, S.; Yu, B.; Zhang, H.; Fei, T.; Zhang, T. Sens. Actuators, B 2014, 202, 272–278. doi:10.1016/j.snb.2014.05.086.

[] Han, M.; Liu, W.; Qu, Y.; Du, L.; Wei, H. J. Mater. Sci.: Mater. Electron. 2017, 28 (22), 16973–16980. doi:10.1007/s10854-017-7619-6.

[] Liu, X.; Cui, J.; Sun, J.; Zhang, X. RSC Adv. 2014, 4 (43), 22601–22605. doi:10.1039/C4RA02453B.

[] Xiao, X.; Zhou, X.; Ma, J.; Zhu, Y.; Cheng, X.; Luo, W.; Deng, Y. ACS Appl. Mater. Interfaces 2019, 11 (29), 26268–26276. doi:10.1021/acsami.9b08128.

[] Singkammo, S.; Wisitsoraat, A.; Sriprachuabwong, C.; Tuantranont, A.; Phanichphant, S.; Liewhiran, C. ACS Appl. Mater. Interfaces 2015, 7 (5), 3077–3092. doi:10.1021/acsami.5b00161.

[] Bagal, L. K.; Patil, J. Y.; Mulla, I. S.; Suryavanshi, S. S. Ceram. Int. 2012, 38 (8), 6171–6179. doi:10.1016/j.ceramint.2012.04.068.

[] Chen, Y.; Yu, L.; Feng, D.; Zhuo, M.; Zhang, M.; Zhang, E.; Xu, Z.; Li, Q.; Wang, T. Sens. Actuators, B 2012, 166-167, 61–67. doi:10.1016/j.snb.2011.12.018.

[] Liu, X.; Zhang, J.; Guo, X.; Wu, S.; Wang, S. Sens. Actuators, B 2011, 152 (2), 162–167. doi:10.1016/j.snb.2010.12.001.

[] Lee, S. C.; Choi, H. Y.; Lee, S. J.; Lee, W. S.; Huh, J. S.; Lee, D. D.; Kim, J. C. Sens. Actuators, B 2009, 138 (2), 446–452. doi:10.1016/j.snb.2009.02.064.

[] Cheng, J. P.; Wang, B. B.; Zhao, M. G.; Liu, F.; Zhang, X. B. Sens. Actuators, B 2014, 190, 78–85. doi:10.1016/j.snb.2013.08.098.

[] Wang, C.; Cui, X.; Liu, J.; Zhou, X.; Cheng, X.; Sun, P.; Hu, X.; Li, X.; Zheng, J.; Lu, G. ACS Sens. 2016, 1 (2), 131–136. doi:10.1021/acssensors.5b00123.

[] Chen, H.; Hu, J.; Li, G.-D.; Gao, Q.; Wei, C.; Zou, X. ACS Appl. Mater. Interfaces 2017, 9 (5), 4692–4700. doi:10.1021/acsami.6b13520.

[] Zhao, S.; Shen, Y.; Zhou, P.; Zhong, X.; Han, C.; Zhao, Q.; Wei, D. Sens. Actuators, B 2019, 282, 917–926. doi:10.1016/j.snb.2018.11.142.

[] Singkammo, S.; Wisitsoraat, A.; Sriprachuabwong, C.; Tuantranont, A.; Phanichphant, S.; Liewhiran, C. ACS Appl. Mater. Interfaces 2015, 7 (5), 3077–3092. doi:10.1021/acsami.5b00161.

[] Zhang, J.; Wu, J.; Wang, X.; Zeng, D.; Xie, C. Sens. Actuators, B 2017, 243, 1010–1019. doi:10.1016/j.snb.2016.12.062.

[] Wang, C.; Zhu, J.; Liang, S.; Bi, H.; Han, Q.; Liu, X.; Wang, X. J. Mater. Chem. A 2014, 2 (43), 18635–18643. doi:10.1039/C4TA03931A.

[] Bhati, V. S.; Ranwa, S.; Rajamani, S.; Kumari, K.; Raliya, R.; Biswas, P.; Kumar, M. ACS Appl. Mater. Interfaces 2018, 10 (13), 11116–11124. doi:10.1021/acsami.7b17877.

[] Cui, S.; Wen, Z.; Mattson, E. C.; Mao, S.; Chang, J.; Weinert, M.; Hirschmugl, C. J.; Gajdardziska-Josifovska, M.; Chen, J. J. Mater. Chem. A 2013, 1 (14), 4462–4467. doi:10.1039/c3ta01673k.

[] Piloto, C.; Shafiei, M.; Khan, H.; Gupta, B.; Tesfamichael, T.; Motta, N. Appl. Surf. Sci. 2018, 434, 126–133. doi:10.1016/j.apsusc.2017.10.152.

[] Wang, Z.; Zhang, Y.; Liu, S.; Zhang, T. Sens. Actuators, B 2016, 222, 893–903. doi:10.1016/j.snb.2015.09.027.

[] Ghosal, S.; Bhattacharyya, P. CSIT 2020, 117–122. doi:10.1007/s40012-020-00299-z.

[] Chen, L.; Huang, L.; Lin, Y.; Sai, L.; Chang, Q.; Shi, W.; Chen, Q. Sens. Actuators, B 2018, 255, 1482–1490. doi:10.1016/j.snb.2017.08.158.

[] Esfandiar, A.; Irajizad, A.; Akhavan, O.; Ghasemi, S.; Gholami, M. R. Int. J. Hydrogen Energy 2014, 39 (15), 8169–8179. doi:10.1016/j.ijhydene.2014.03.117.