Supporting Information 
for

Synthesis of novel multifunctional carbazole based molecules, their thermal, electrochemical and optical properties

Nuray Altinolcek1, Ahmet Battal2,3, Mustafa Tavasli1*, William J. Peveler3, Holly A. Yu3 and Peter J. Skabara3

Address: 1Department of Chemistry, Faculty of Science-Art, Uludag University, 16059 Nilufer, Bursa, Turkey, 2Department of Elementary School Education, Faculty of Education, Mus Alparslan University, 49100, Mus, Turkey and 3WestCHEM, School of Chemistry, University of Glasgow, Joseph Black Building, G128QQ Glasgow UK.

Email: Mustafa Tavaslı*  - mtavasli@uludag.edu.tr

* Corresponding author

NMR, FTIR, MS and HRMS spectra of compounds and relative quantum yield calculations

Table of contents

| - 1H and 13C NMR Spectra | Figure S1: | 1H NMR spectrum of 3-bromocarbazole (2) | SI-3 |
| --- | --- | --- | --- |
|  | Figure S2: | 1H NMR spectrum of 3-bromo-N-hexylcarbazole (4) | SI-3 |
|  | Figure S3: | 1H NMR spectrum of N-hexylcarbazole-3-yl-boronic acid pinocolate ester (5) | SI-4 |
|  | Figure S4: | 1H NMR spectrum of compound 7a | SI-4 |
|  | Figure S5: | 13C NMR spectrum of compound 7a | SI-5 |
|  | Figure S6: | 1H NMR spectrum of compound 7b | SI-5 |
|  | Figure S7: | 13C NMR spectrum of compound 7b | SI-5 |
| - FT-IR Spectra | Figure S8: | FT-IR spectrum of compounds 7a and 7b | SI-6 |
| - Mass and HRMS Spectra | Figure S9: | Mass spectrum of compound 7b | SI-6 |
|  | Figure S10: | HRMS result of compound 7b | SI-6 |
| - Calculations of Relative Fluorescence Quantum Yields | Figure S11: | Absorption at 355 nm-Integrated Emission of samples (7a and 7b) and reference (Rhodamine B) | SI-7 |
|  | Table S1: | Optical density and integrated PL intensity values of reference (Rhodamine B) and samples (7a and 7b) | SI-8 |
|  | Figure S12: | Absorption spectra of Rhodamine B, 7a and 7b | SI-8 |
|  | Figure S13: | Emission (PL) spectra of Rhodamine B, 7a and 7b, excited at 355 nm | SI-8 |

- 1H and 13C NMR Spectra

Figure S1: 1H NMR spectrum of 3-bromocarbazole (2).

Figure S2: 1H NMR spectrum of 3-bromo-N-hexylcarbazole (4)

Figure S3: 1H NMR spectrum of N-hexylcarbazole-3-yl-boronic acid pinocolate ester (5)

Figure S4: 1H NMR spectrum of compound 7a

Figure S5: 13C NMR spectrum of compound 7a

Figure S6: 1H NMR spectrum of compound 7b

Figure S7: 13C NMR spectrum of compound 7b

- FT-IR Spectra

Figure S8: FT-IR spectrum of compounds 7a and 7b

- Mass and HRMS Spectrum

Figure S9: Mass spectrum of compound 7b

Figure S10: HRMS result of compound 7b

- Calculations of Relative Fluorescence Quantum Yields

Relative fluorescent quantum yields of samples (S) were calculated from Figure S11 by using equation 1, where yS is the integrated fluorescence intensity of samples (7a/7b), yR is the integrated fluorescence intensity of reference (Rhodamine B), n is the refractive index of solvents used.

s=yS.RyR.ns2nr21

Figure S11, plotted from Table S1, depicts absorption at 355 nm (OD, optical density) versus integrated emission (integrated fluorescence intensity of reference and samples).

For this, samples (7a and 7b) were dissolved in dichloromethane (n=1.435) and reference (Rhodamine B) was dissolved in absolute ethanol (n=1.361). Different concentrations of reference (C1-C7) and samples (7a: C1-C5 and 7b: C1-C8) were then prepared. For each concentration absorption spectra of reference and samples were recorded as depicted in Figure S12. Both reference and samples were excited at 355 nm, then emission spectra of reference and samples were recorded as depicted in Figure S13. All of these values are summarised in Table S1.

Figure S11: Absorption at 355 nm-Integrated Emission of samples (7a and 7b) and reference (Rhodamine B)

| Table S1: Optical density and integrated PL intensity values of reference (Rhodamine B) and samples (7a and 7b) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Rhodamine B |  |  | 7a |  |  | 7b |  |  |
| (exc= 355 nm) |  |  | (exc= 355 nm) |  |  | (exc= 355 nm) |  |  |
| Unsorted | OD (a.u) | Integrated PL intensity (a.u) | Unsorted | OD (a.u) | Integrated PL intensity (a.u) | Unsorted | OD (a.u) | Integrated PL intensity (a.u) |
| C1 | 0.00873 | 37591.15917 | C1 | 0.02143 | 14075.26276 | C1 | 0.03855 | 312854.9439 |
| C2 | 0.00849 | 35459.07801 | C2 | 0.03538 | 20063.43206 | C2 | 0.03810 | 307049.5385 |
| C3 | 0.00804 | 33547.29896 | C3 | 0.04274 | 28371.31840 | C3 | 0.03599 | 297563.9041 |
| C4 | 0.00786 | 33095.41848 | C4 | 0.06100 | 35022.74323 | C4 | 0.03441 | 286229.5682 |
| C5 | 0.00762 | 31942.84488 | C5 | 0.07916 | 41000.28228 | C6 | 0.03284 | 256749.5341 |
| C6 | 0.00734 | 30932.30389 |  |  |  | C7 | 0.02933 | 240013.4747 |
| C7 | 0.00726 | 29668.39935 |  |  |  | C8 | 0.02770 | 218127.6961 |
| Gradient=PL/OD |  | 4,793,252.39 | Gradient=PL/OD |  | 474,455.83 | Gradient=PL/OD |  | 8,579,616.58 |
| Refractive index of ethanol |  | 1.361 | Refractive index of dichloromethane |  | 1.435 | Refractive index of dichloromethane |  | 1.435 |
| PLQY | 0.49 |  | PLQY | 0.054 |  | PLQY | 0.974 |  |
| Unit PLQY | 1.02227E-07 |  | Estimated error on values ca. ± 10% RSD. |  |  |  |  |  |

Figure S12: Absorption spectra of Rhodamine B, 7a and 7b

Figure S13: Emission (PL) spectra of Rhodamine B, 7a and 7b, excited at 355 nm.