Appendix

Table A. Required values for the theoretical models and the resulting interfacial energies “by wetting angle”, “by van der Waals energies” and “according to the R. H. Ewing”.

|  | RT (25°C) |  |  |  | 400°C |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Silicon oxide | Gold |  | Silicon |  | Silicon oxide | Gold |  | Silicon |  |
| Hamaker constant Aij [10-19 J][1–9] | 3.08 – 9.96 |  |  |  | 3.08 – 9.96 |  |  |  |  |
|  |  | 2.90 – 6.43 |  |  |  |  | 2.90 – 6.43 |  |  |  |
|  |  | 2.81 – 5.29 |  |  |  |  | 2.81 – 5.29 |  |  |  |
| Surface energy [J/m2] | 0.01 [10] | 1.26 [11] |  | 1.23 [12] |  | 0.01 [10] | 1.20 [11] |  | 1.23 [12] |  |
| Wetting angle | 84° |  |  |  | 84° |  |  |  |  |
|  |  | 42° |  |  |  |  | 42° |  |  |  |
| energetic portion in interfacial energy [13] | 0.155 | -0.018 |  | 0.286 |  | 0.155 | -0,041 |  | 0.285 |  |
| Particle diameter [nm] |  | 0.35 [14] |  |  |  |  | 0.35 [14] |  |  |  |
| Interfacial energy WA [J/m2] | -0,03 |  |  |  | -0,03 |  |  |  |  |
|  |  | 0,29 |  |  |  |  | 0,34 |  |  |  |
| Interfacial energy VW[J/m2] | -1.35 |  |  |  | -1,28 |  |  |  |  |
|  |  | 0,09 |  |  |  |  | 0,16 |  |  |  |
| Interfacial energy AE [J/m2] | 0.14 |  |  |  | 0.11 |  |  |  |  |
|  |  | 0.27 |  |  |  |  | 0.24 |  |  |  |

# References

1.	Krupp, H. Adv. Colloid Interface Sci. 1967, 1 (2), 111–239

2.	Visser, J. Adv. Colloid Interface Sci. 1972, 3 (4), 331–363

3.	Schwerdtfeger, P. Cent. Theor. Chem. Physics, Massey Univ. 2015

4.	Buttner, F. H.; Udin, H.; Wulff, J. JOM 1951, 3 (12), 1209–1211

5.	Paradisa, P. F.; Ishikawaa, T.; Koikeb, N. Gold Bull. 2008, 41 (3), 242–245

6.	Kim, J. Y.; Hwang, M. S.; Kim, Y.-H.; Kim, H. J.; Lee, Y. J. Appl. Phys. 2001, 90 (5), 2469–2473

7.	Bettin, H.; Toth, H. IEEE Trans. Instrum. Meas. 2007, 56 (2), 257–261

8.	Biggs, S.; Mulvaney, P. J. Chem. Phys. 1994, 100 (11), 8501–8505

9.	Bergström, L. Adv. Colloid Interface Sci. 1997, 70, 125–169

10.	Janssen, D.; De Palma, R.; Verlaak, S.; Heremans, P.; Dehaen, W. Thin Solid Films 2006, 515 (4), 1433–1438

11.	Egry, I.; Lohoefer, G.; Jacobs, G. Phys. Rev. Lett. 1995, 75 (22), 4043

12.	Jaccodine, R. J. J. Electrochem. Soc.  1963, 110 (6), 524–527

13.	Jones, H. Mater. Lett. 2002, 53 (4–5), 364–366

14.	Clementi, E.; Raimondi, D. L.; Reinhardt, W. P. J. Chem. Phys. 1967, 47 (4), 1300–1307