Supporting Information

Figure S1. The high resolution mass spectra of PI-Cz

Figure S2. The 1H NMR spectrum of PI-Cz in DMSO-d6.

Table S1. Crystal data and structure refinement forPI-Cz

| Compound | PI-Cz |
| --- | --- |
| Empirical formula | C33H22N2O2 |
| Formula weight | 478.52 |
| Temperature/K | 220.00(10) |
| Crystal system | monoclinic |
| Space group | P21/c |
| a/Å | 8.6894(2) |
| b/Å | 35.8672(5) |
| c/Å | 8.10020(10) |
| α/° | 90 |
| β/° | 107.351(2) |
| γ/° | 90 |
| Volume/Å3 | 2409.67(8) |
| Z | 4 |
| ρcalcg/cm3 | 1.319 |
| μ/mm-1 | 0.653 |
| F(000) | 1000.0 |
| Crystal size/mm3 | 0.23 × 0.15 × 0.04 |
| Radiation | CuKα (λ = 1.54184) |
| 2Θ range for data collection/° | 9.864 to 146.646 |
| Index ranges | -10 ≤ h ≤ 9, -43 ≤ k ≤ 40, -9 ≤ l ≤ 6 |
| Reflections collected | 7798 |
| Independent reflections | 4617 [Rint = 0.0301, Rsigma = 0.0400] |
| Data/restraints/parameters | 4617/0/335 |
| Goodness-of-fit on F2 | 0.997 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0489, wR2 = 0.1351 |
| Final R indexes [all data] | R1 = 0.0544, wR2 = 0.1427 |